Table 1. Model Performance Benchmarking

| Model | Test R² | RMSE (eV) | MAE (eV) | CV R² (5-fold) | CV σ |
| --- | --- | --- | --- | --- | --- |
| Extra Trees (highest R²) | 0.7414 | 0.2267 | 0.1529 | 0.6996 | 0.0947 |
| Random Forest | 0.7116 | 0.2395 | 0.1655 | 0.6952 | 0.0750 |
| Gradient Boosting (SHAP) | 0.7197 | 0.2360 | 0.1699 | 0.6614 | 0.1028 |
| SVR-RBF | 0.5024 | 0.3145 | 0.1991 | 0.6762 | 0.0821 |
| Lasso | 0.5552 | 0.2973 | 0.2292 | 0.4735 | 0.0549 |
| Ridge | 0.5539 | 0.2978 | 0.2298 | 0.4674 | 0.0566 |
| ElasticNet | 0.5547 | 0.2975 | 0.2293 | 0.4744 | 0.0523 |

Table 2. Noise Floor vs. Model Performance

| Quantity | Value (eV) |
| --- | --- |
| Tauc-plot single-lab noise | 0.075 |
| GB MAE, full dataset (N = 638) | 0.1699 |
| Median inter-paper σ, repeated pairs | 0.1783 |
| Mean inter-paper σ, repeated pairs | 0.2491 |
| GB RMSE, full dataset | 0.2360 |
| 90th-percentile inter-paper σ | 0.5838 |
| GB MAE, clean subset (N ≈ 566) | 0.1171 |
| GB RMSE, clean subset | 0.1595 |

Table 3. High-Variance Host–Dopant Pairs (σ > 0.40 eV)

| Host | Dopant | N papers | N rows | σ (eV) | Range (eV) |
| --- | --- | --- | --- | --- | --- |
| SnO2 | Co | 4 | 17 | 0.8009 | 1.8814 |
| In2O3 | Sn | 2 | 8 | 0.7336 | 1.0375 |
| SnO2 | Cu | 2 | 8 | 0.7248 | 1.0250 |
| WO3 | V | 3 | 6 | 0.6195 | 1.1525 |
| ZnO | W | 2 | 7 | 0.5798 | 0.8200 |
| WO3 | Al | 2 | 4 | 0.5185 | 0.7333 |
| CeO2 | Gd | 3 | 14 | 0.4971 | 0.9942 |
| CeO2 | Fe | 3 | 8 | 0.4967 | 0.9933 |

Table 4. Gradient Boosting Performance: Full vs. Clean Subset

| Metric | Full dataset (N = 638) | Clean subset (N ≈ 566) | Change |
| --- | --- | --- | --- |
| Test R² | 0.7197 | 0.8291 | +0.1093 |
| RMSE (eV) | 0.2360 | 0.1595 | -0.0765 |
| MAE (eV) | 0.1699 | 0.1171 | -0.0529 |
| CV-R² (5-fold) | 0.661 ± 0.103 | 0.685 ± 0.051 | +0.024 |

Table 5. Per-Host Within-Paper Concentration-Sensitivity

| Host | N series | Pearson r | p-value | Sign agr. (%) |
| --- | --- | --- | --- | --- |
| TiO2 | 17 | 0.997 | <0.001 | 88.2% |
| CeO2 | 25 | 0.895 | <0.001 | 92.0% |
| SnO2 | 20 | 0.842 | <0.001 | 75.0% |
| ZnO | 20 | 0.842 | <0.001 | 75.0% |
| WO3 | 21 | 0.715 | <0.001 | 76.2% |
| In2O3 | 16 | -0.068 | 0.801 | 56.2% |
| Overall | 119 | 0.837 | 0.000 | 78.2% |

Table S1. Key Computed Metrics (Supplementary Reference)

| Metric | Value |
| --- | --- |
| Extra Trees Test R² | 0.7414 |
| Extra Trees RMSE (eV) | 0.2267 |
| Extra Trees MAE (eV) | 0.1529 |
| Extra Trees CV R² ± σ | 0.6996 ± 0.0947 |
| GB Test R² | 0.7197 |
| GB RMSE (eV) | 0.2360 |
| GB MAE (eV) | 0.1699 |
| GB CV R² ± σ | 0.6614 ± 0.1028 |
| Conformal q₉₀ half-width (eV) | 0.3858 |
| Conformal full interval width (eV) | 0.7717 |
| Conformal empirical coverage | 89.8% |
| Conformal finite-sample guarantee | ≥89.0% |
| Conformal Nᴄᴀʟ | 102 |
| GB residual mean (eV) | 0.0195 |
| GB residuals within ±0.10 eV | 42.2% |
| GB residuals within ±0.20 eV | 72.7% |
| Clean-subset R² (GB) | 0.8291 |
| Clean-subset RMSE (eV) (GB) | 0.1595 |
| Clean-subset MAE (eV) (GB) | 0.1171 |
| Clean-subset CV-R² ± σ (GB) | 0.6850 ± 0.0506 |
| Within-paper slope r, all series | 0.837 |
| Within-paper slope r, mixed series | 0.234 |
| Mixed-series p-value | 0.048 |
| Within-paper slope r, train-only | 0.988 |
| Sign agreement, all series | 93/119 (78.2%) |